## Slide 1: Trap analysis Validity of Hurkx trap-assisted tunneling
Student : Ying-Lun Kao
Advisor : Dr. Hao-Hsiung Lin
Date : 108. 09. 25

## Slide 2
Abstract
Trap-assisted tunneling 關鍵在於 tunneling probability。已知三種 Field-enhanced thermal emission model，前兩種結果相同，但與第三種差異在 pre-factor。第一種為 Hurkx 使用的 Effective-mass approximation，據我推測可能僅適用足夠小的材料跨壓。第二種為 Korol 針對深能井所使用的 Green‘s function approach。第三種為 W. W. Anderson 使用的 Oppenheimer approach，適用深能井。由於時間有限，目前僅分析 Hurkx validity，並對不同跨壓範圍擬合分析，討論可能誤差來源。
針對 InP，不論跨壓都有不錯 IV 擬合，並有深能井 且 ，文獻值約。針對 InGaAs，不論跨壓皆有不錯 IV 擬合，並能驗證羅博士提供的 APD 濃度，成功解釋擊穿電流之緩慢上升現象，，其 SRH lifetime 也大致保有 級數規律，等效質量約 ，文獻值約。

## Slide 3
Outline
SRH recombination model
Field-enhanced thermal emission rate model
Curve fitting method
Fitting results

## Slide 4: SRH recombination model
Approximation of SRH recombination rate
SRH recombination current equation

## Slide 5
Pure SRH recombination rate

## Slide 8
For

## Slide 9
SRH recombination current equation

## Slide 10: Field-enhanced thermal emission rate model
Hurkx model: Effective-mass approximation
Korol model: Green’s function approach (Quantum field theory & self energy)
W. W. Anderson model: Oppenheimer approach

## Slide 11
Effective-Mass Approximation (EMA)
Without periodic potential
In periodic & external potential
Classical E.O.M. :
Schrödinger’s equation :
General Hamiltonian equation :
Semi-classical E.O.M. :
Effective-mass equation :
General Hamiltonian equation in periodic lattice potential :

## Slide 12
Two complete sets of orthogonal functions
The Bloch function
The Wannier function

## Slide 13
Expansion in Wannier functions
Assuming using only wave functions from single band is justifiable, i.e., , , we drop the index n and the factor is introduced for normalization.
If is a slowly varying function of , it may be regarded as an amplitude determining the magnitude of the wave function in the jth unit cell, since falls off rapidly outside this cell.
behaves like a
normalized wave function

## Slide 14
Differential equation for the amplitude function
We now seek to solve the wave equation, , where is the Hamiltonian for the perfect crystal and is a slowly varying perturbing potential. After plugging , we then multiply by and integrate over the volume . Then we obtain the equations:
since is a slowly varying function
Re-ordering
index j

## Slide 15
Differential equation for the amplitude function
,
Question : How to find ?
Answer : Solve the following “new” equation and set successively in the slowly varying function .
But how?
The dispersion relation of perfect crystal:
If ,

## Slide 16
Hurkx TAT model: Linearly varying potential
,
(not parabolic)
Let , where

## Slide 17
General SRH+TAT expression:

## Slide 18
Phonon-assisted tunneling:
Let ,
Is it plausible?

## Slide 19
General SRH+TAT expression:
Let ,

## Slide 20
For not too large field, e.g., at room temperature and for , ,
In sum,
For uniform doping concentration,

## Slide 21
Validity of Hurkx trap-assisted tunneling model
,
(not parabolic)
Single-band approximation
Spherical & parabolic band approximation
因為 InP 的 valley 質量並不大，以及InP 電場特別高，所以電子很容易有高能量，也就容易產生 intervalley scattering，使得上述近似並不適用於 InP。而即便僅有 intravalley scattering，這時也必須考慮能帶的 nonparabolicity，使得等效質量之 Hamiltonian 將十分複雜。而 InGaAs 之電場較小，所以應該較適合 spherical & parabolic band。

## Slide 22
InGaAs
EMA confident interval

## Slide 24
valley:
valley:
valley:
 | valley | valley | valley
# of valleys | 1 | 4 | 3
Nonparabolicity | 1.0 | 0.4 | 0.5
Effective mass | 0.08 |  | 
longitudinal |  | 0.95 | 0.9
transverse |  | 0.32 | 0.3
Valley separation |  | 0.54 | 0.78
# of valleys | 1 | 4 | 3
Nonparabolicity | 1.0 | 0.4 | 0.5
Effective mass | 0.08 |  | 
longitudinal |  | 0.95 | 0.9
transverse |  | 0.32 | 0.3
Valley separation |  | 0.54 | 0.78
Band structure
valley:
InGaAs:
InP

## Slide 26
Curve fitting method
Setting TCAD Doping Profile
Zn diffusion
Distribution
InP maximum field
Least square method
Find best trap level, effective mass and lifetime
Charge layer
InGaAs maximum field
Depletion width

## Slide 27: Fitting results
2 Doping profiles ( or )
IV, trap, effective mass and lifetime results
  Large bias range &
  Small bias range &
  Large bias range &
  Small bias range &

## Slide 28
游朝政論文內容截圖
7.8e16
2e17
5e16
7.5e14
2e15
Multiplication layer: 0.42 μm
Charge layer: 0.2 μm
Grading layer: 0.12 μm
Absorption layer: 3 μm

## Slide 29
0917/IV_fitting.py

## Slide 30
0917/IV_ABthick1.py

## Slide 31
0917/IV_fitting.py

## Slide 32
0917/IV_ABthick1_beta.py

## Slide 33
0917/IV_fitting.py

## Slide 34
0917/IV_fitting.py

## Slide 35
0917/IV_ABthick1.py

## Slide 36
0917/IV_ABthick1_beta.py

## Slide 37
0917/IV_fitting.py

## Slide 38
0917/IV_fitting.py

## Slide 39
0917/IV_ABthick1.py

## Slide 40
0917/IV_ABthick1_beta.py

## Slide 41
Discussions
Why do we rule out SRH without trap-assisted tunneling?
Validity of effective-mass approximation
Dependence of effective mass, lifetime and trap level
Doping effects
  Uncertainty effect of grading layer concentration ()
  Depletion width and equivalent depletion width distribution
  Overestimation of Hurkx trap-assisted tunneling when

## Slide 42
Assumptions about device parameters